SUPPORTING INFORMATION

Temperature invariant, nearly zero temperature coefficient of

resistivity in Si-doped titanium nitrides

S. Novia Berriel,1 Corbin Feit,1 Md. Rafiqul Islam,2 Jia Shi,3 Somilkumar J. Rathi,4 Ajit Dhamdhere,4 Hae Young Kim,4 Patrick E. Hopkins,2,5,6 Talat Rahman,3,7 Duy Le,3,7 Parag Banerjee* 1,7,8,9

1Department of Materials Science and Engineering, University of Central Florida, Orlando, FL 32816 USA.

2Department of Mechanical Engineering and Aerospace Engineering, University of Virginia, Charlottesville, VA 22904 USA.

3Department of Physics, University of Central Florida, Orlando, FL 32816 USA.

4Eugenus, Inc., 677 River Oaks Parkway, San Jose, CA, 95134, USA.,

5Department of Materials Science and Engineering, University of Virginia, Charlottesville, Virginia 22904 USA.

6Department of Physics, University of Virginia, Charlottesville, Virginia 22904 USA.

7REACT Faculty Cluster, University of Central Florida, Orlando, Florida 32816 USA.

8Nano Science and Technology Center, University of Central Florida, Orlando, Florida 32816 USA.

9 Florida Solar Energy Center, University of Central Florida, Orlando, Florida 32816 USA.

*Corresponding authors: parag.banerjee@ucf.edu

# Supporting Information S1: Density functional theory (DFT) calculations of potential effects of Si and O in the Ti-Si-N lattice

Figure S1. Structural unit of 21 supercells used for calculating the band structure of Ti-Si-N-O system.

Density functional theory calculations were conducted to search possible Si placement in TiN lattice which would significantly affect the electronic properties of TiN. In the trial configurations considered, a Si atom was either placed on a Ti or N lattice site, replacing a Ti or N, respectively. Additionally, since it was known that the films had O, one or two O atoms were placed either interstitially or by replacing a N from its lattice site. All calculations were performed with either a (2×2×2) or (3×3×3) TiN supercell. These various permutations of Si and O placement resulted in a total of 21 different configurations. The structures are graphically summarized here in Figure S1.

In Table S1, we show results of the electronic structure calculations, using GGA and GGA+U approaches, for the 21 structures considered in this work. First, it was verified that TiN (i.e., Ti8N8) band structure calculations yield results corresponding to those reported in literature.[1] Owing to the strong Coulomb repulsion between 3d electrons of transition metal Ti, GGA + U method is capable of providing a more accurate description of electronic properties compared to GGA.[2-3] Here, the U value is adopted as 4.4 eV, which has been proven to successfully correct the local states of 3d electron in Ti.[4-5] The band structure for TiN indicates that TiN behaves as a metal i.e., with no band gap.

In total, 17 band structure calculations yielded metallic behavior with no band gap formation. Only one structure (structure # 20, N8Ti7Si1O2) predicted a semiconductor with a definite band gap opening. Two configurations resulted in band gap opening while maintaining a finite DOS at the Fermi level. These correspond to structure # 8, N8Ti7SiO, structure # 9 N7Ti7SiO2 in Table S1, and collectively the above three configurations, their DOS and band structures are shown in Figure S2.

Specifically in these cases, a Si atom substitutes a Ti atom and one, or two, O atoms are located interstitially or substitute in the neighboring N site. The structures have a commonality, in that a Si-O bond exists in the unit cell. We also importantly note that the presence of a Si-O bond does not necessarily produce a gap / semiconductor behavior.

| # | Structure Unit | GGA | GGA+ U |
| --- | --- | --- | --- |
| 1 | N8Ti8 | Metal | Metal |
| 2 | N8Ti7Si1 | Metal | - |
| 3 | N6Ti8O2 | Metal | Metal |
| 4 | N7Ti8O1 | Metal | Metal |
| 5 | N6Ti7Si1O2 | Metal | Metal |
| 6 | N7Ti7Si1O1 (Si bonding with O) | Metal | Metal |
| 7 | N7Ti7Si1O1 (Si NOT bonding with O) | Metal | - |
| 8 | N8Ti7Si1O1 | Metal | Metal |
| 9 | N7Ti7Si1O2 | Metal | Metal |
| 10 | N27Ti27 | Metal | - |
| 11 | N27Ti26Si1 | Metal | - |
| 12 | N27Ti26Si1O1 | Metal | - |
| 13 | N26Ti27O1 | Metal | - |
| 14 | N26Ti26Si1O1 (Si bonding with O) | Metal | - |
| 15 | N26Ti26Si1O1 (Si NOT bonding with O) | Metal | - |
| 16 | N25Ti26Si1O2 | Metal | - |
| 17 | N8Ti8O1 | Metal | - |
| 18 | N8Ti8O2 | Metal | - |
| 19 | N8Ti7Si1O2 (Si NOT bonding with O) | Metal | - |
| 20 | N8Ti7Si1O2 (Si bonding with one O) | Semiconductor | - |
| 21 | N8Ti7Si1O2 (Si bonding with two O) | Metal | - |

Table S1. Formula unit used for DFT and calculation results using GGA and GGA + U. Calculations from the bolded structures show band gap opening, though the bolded “metal” categorization indicates a finite density of states at the Fermi level as shown in Figure S2.

Figure S2. (A) – (C) Structure unit, DOS and E vs. k for N8Ti7SiO, respectively. (D) – (F) Structure unit, DOS and E vs. k for N7Ti7SiO2, respectively and (G) – (I) Structure unit, DOS and E vs. k for N8Ti7SiO2, respectively.

# Supporting Information S2: Thermal Conductivity Analysis

The temperature-dependent thermal conductivities of Ti1-xSixN films were measured using a time-domain thermoreflectance (TDTR) technique. To verify TDTR measurements are sensitive to cross-plane thermal conductivity of Ti1-xSixN films, a sensitivity analysis was performed. TDTR sensitivity was calculated to cross-plane thermal conductivity of each film stack. Various thermophysical properties of each layer are listed in Table S2 below.

| Material | Thickness (nm) | Room temperature heat capacity, MJm-3K-1 | Thermal conductivity, W m-1 K-1 | Thermal boundary resistance, (TBR) m2 K GW-1 |
| --- | --- | --- | --- | --- |
| Al | 80 | 2.42 [2] | 144 |  |
| Al/Ti1-xSixN | -- | -- | -- | TDTR best fit valuesb |
| TiN | 142.3 | 2.95 [11,12] |  |  |
| Ti0.98Si0.2N | 119.1 | 3.05 [11–14] |  |  |
| Ti0.914Si0.086N | 139 | 3.42 [11–14] |  |  |
| Ti0.758Si0.242N | 136 | 3.29 [11–14] |  |  |
| Ti1-xSixN/SiO2 |  |  |  | 10.00 [4] |
| SiO2 | 100 | 1.62 [1,3,4] | 1.35 [1,2,4,5] |  |
| SiO2/Si | - | - | - | 4.35 [3,4] |
| Si | - | 1.65 [1–5] | 130 [1,4] | - |

Table S2: Parameters used in sensitivity analysis and thermal model to determine the cross-plane thermal conductivity of Ti1-xSixN films for room temperature measurements. Here, we derived the electrical thermal conductivity of Al from the 4 point-probe measured electrical resistivity applying Wiedemann-Franz Law assuming the low temperature value of the Lorenz number (2.44x10-8 ΩWK-2). The thickness of Al is 80 nm determined by picosecond ultrasonic measurements.[6-7] The heat capacity at different temperatures for Ti1-xSixN was determined using rule of mixtures applied on the heat capacity[8-11] of  TiN and Si3N4. The temperature-dependent thermal conductivity and heat capacity  of Al, SiO2, and  Si as a function of temperature were taken from the literature[12-13].

Figure S3 shows that our measurement has sufficient sensitivity to the cross-plane thermal conductivity of Ti1-xSixN films, provided knowledge of the thermal conductivity of the SiO2 layer in the substrate. Therefore, the accepted literature values[14-18] for SiO2 could be used in our thermal model to fit the experimental data and perform uncertainty calculations on this assumption as discussed in the following section. To determine the thermal conductivity of Ti1-xSixN films, we employ a four-layer heat diffusion model[19-21]. Figure 1b exhibits the best-fit thermal model to the ratio of the in-phase and out-of-phase signal (–Vin/Vout) fitting for the thermal conductivity of Ti1-xSixN films and thermal boundary resistance of Al/ Ti1-xSixN. To fit the experimental data with the model we use the thermophysical properties of Al, Ti1-xSixN, SiO2 and Si listed in Table S2.

Figure S3: (a) Sensitivity of TDTR measurements to the ratio of in-phase to out-of-phase signal (-Vin/Vout) for the cross-plane thermal conductivities (κ). (b) Theoretical fit of TDTR experimental data for TiN, Ti0.98Si0.02N, Ti0.914Si0.086N and Ti0.758Si0.242N films obtained at room temperature.

We calculate the total uncertainty (i) using the following equation[14, 22],

i= (σi2)+i∆i2)        Eq. S1

Here i represents the standard deviations among multiple measurements across various spots and ∆i is the uncertainty associated with an individual parameter of the thermal model. The uncertainty of TDTR measurements include the thermal conductivity variations at different spots for multiple measurements, the thickness of Al, Ti1-xSixN and SiO2 (± 3%) and volumetric heat capacity of Ti1-xSixN (± 5%), the thermal conductivity of Al and SiO2 (±10%) and thermal boundary resistance of Ti1-xSixN/SiO2 (± 900%).

References

[1]	M. Marlo, V. Milman, Phys. Rev. B 2000, 62, 2899.

[2]	B. Himmetoglu, A. Floris, S. de Gironcoli, M. Cococcioni, International Journal of Quantum Chemistry 2014, 114, 14.

[3]	E. R. Ylvisaker, W. E. Pickett, K. Koepernik, Phys Rev B 2009, 79, 035103.

[4]	B. J. Morgan, G. W. Watson, Surface Science 2007, 601, 5034.

[5]	E. Finazzi, C. Di Valentin, G. Pacchioni, A. Selloni, The Journal of Chemical Physics 2008, 129, 154113.

[6]	C. Thomsen, H. J. Maris, J. Tauc, Thin Solid Films 1987, 154, 217.

[7]	C. Thomsen, J. Strait, Z. Vardeny, H. J. Maris, J. Tauc, J. J. Hauser, Physical Review Letters 1984, 53, 989.

[8]	W. Lengauer, S. Binder, K. Aigner, P. Ettmayer, A. Guillou, J. Debuigne, G. Groboth, Journal of Alloys and Compounds 1995, 217, 137.

[9]	A. Seifitokaldani, A. E. Gheribi, M. Dollé, P. Chartrand, Journal of Alloys and Compounds 2016, 662, 240.

[10]	A. Kuwabara, K. Matsunaga, I. Tanaka, Phys Rev B 2008, 78.

[11]	N. Nishiyama, S. Kitani, Y. Ohta, E. Kulik, Z. Netriová, A. Holzheid, Z. Lenčéš, H. Kawaji, F. Wakai, Journal of the European Ceramic Society 2020, 40, 6309.

[12]	Y. S. Touloukian, E. Buyco, Specific heat - metallic elements and alloys. (Reannouncement). Data book, Vol. 4, United States.

[13]	Y. S. Touloukian, R. W. Powell, C. Y. Ho, P. Klemens, Thermal conductivity - metallic elements and alloys. (Reannouncement). Data book, Vol. 1, United States.

[14]	J. L. Braun, D. H. Olson, J. T. Gaskins, P. E. Hopkins, Review of Scientific Instruments 2019, 90, 024905.

[15]	C. Cancellieri, E. A. Scott, J. Braun, S. W. King, R. Oviedo, C. Jezewski, J. Richards, F. La Mattina, L. P. H. Jeurgens, P. E. Hopkins, Journal of Applied Physics 2020, 128, 195302.

[16]	J. L. Braun, C. H. Baker, A. Giri, M. Elahi, K. Artyushkova, T. E. Beechem, P. M. Norris, Z. C. Leseman, J. T. Gaskins, P. E. Hopkins, Phys Rev B 2016, 93, 140201.

[17]	M. S. B. Hoque, Y. R. Koh, K. Aryana, E. R. Hoglund, J. L. Braun, D. H. Olson, J. T. Gaskins, H. Ahmad, M. M. M. Elahi, J. K. Hite, Z. C. Leseman, W. A. Doolittle, P. E. Hopkins, Review of Scientific Instruments 2021, 92, 064906.

[18]	E. A. Scott, S. W. Smith, M. D. Henry, C. M. Rost, A. Giri, J. T. Gaskins, S. S. Fields, S. T. Jaszewski, J. F. Ihlefeld, P. E. Hopkins, Applied Physics Letters 2018, 113, 192901.

[19]	D. G. Cahill, K. Goodson, A. Majumdar, Journal of Heat Transfer 2002, 124, 223.

[20]	P. E. Hopkins, J. R. Serrano, L. M. Phinney, S. P. Kearney, T. W. Grasser, C. T. Harris, Journal of Heat Transfer 2010, 132, 081302.

[21]	D. G. Cahill, Review of Scientific Instruments 2004, 75, 5119.

[22]	J. P. Feser, D. G. Cahill, Review of Scientific Instruments 2012, 83, 104901.